### Steel Fiber Reinforced Concrete Project

The Concrete Materials Research Institute (CMRI) , at the San Diego State University, Civil and Environmental Engineering Department, has performed the following laboratory testing on mix design 813865P supplied by San Diego Ready Mix Concrete , utilized in the Steel Fiber Reinforced Concrete Project (SFRC).  The 1” DRAMIX® steel fiber was supplied by the manufacturer N.V. BEKAERT S.A.

### Laboratory Testing of Concrete Cylinders

The Laboratory testing of all cylinders fabricated at the project was conducted in accordance with the requirements of ASTM C192 "Making and Curing Concrete Test Specimens in the Laboratory”, and ASTM C39 "Standard Test Method for Cylindrical Concrete Specimens".  Test results are provided in the following Table.

#### Compressive Strength: Plain Concrete

| Specimen - Plain Concrete | P1 | P2 |  |  | P3 |
| --- | --- | --- | --- | --- | --- |
| Date Made | 12-Jun-2000 | 12-Jun-2000 |  |  | 12-Jun-2000 |
| Date Tested | 10-Jul-2000 | 10-Jul-2000 |  |  | 10-Jul-2000 |
| Concrete Age Tested, days | 28 | 28 |  |  | 28 |
| Maximum Load, lbs | 96,000 | 100,000 |  |  | 96,000 |
| Average Compressive Strength, psi | 3,460 | 3,530 |  |  | 3,390 |
| Average Compressive Strength, psi | 3,460 |  |  |  |  |

#### Compressive Strength: Steel Fiber Reinforced Concrete

| Specimen – Steel Fiber Reinforced Concrete | SF1 | SF2 |  |  | SF3 |
| --- | --- | --- | --- | --- | --- |
| Date Made | 12-Jun-2000 | 12-Jun-2000 |  |  | 12-Jun-2000 |
| Date Tested | 10-Jul-2000 | 10-Jul-2000 |  |  | 10-Jul-2000 |
| Concrete Age Tested, days | 28 | 28 |  |  | 28 |
| Maximum Load, lbs | 83,000 | 102,000 |  |  | 90,000 |
| Average Compressive Strength, psi | 2,930 | 3,600 |  |  | 3180 |
| Average Compressive Strength, psi | 3,240 |  |  |  |  |

### Laboratory Testing of Concrete Beams

The Laboratory testing of all beams fabricated at the project were conducted in accordance with ASTM C192 "Making and Curing Concrete Test Specimens in the Laboratory”.  Testing was conducted by M. Ziad Bayasi, Ph.D., S.E., P.E.  Results of the testing can be found in the attached Laboratory Testing of Concrete Beams Supplement.

1)  M. Ziad Bayasi, Ph.D, S.E., P.E., Associate Professor in charge of CMRI, Janusz Supernak, Ph.D, Department Chairman, Fang H. Chou, Ph.D, P.E., Advisor  and Assistant Dean.

2) The San Diego Ready Mix Concrete Company is a Division of Superior Ready Mix Concrete, L.P.  The supply of concrete material was made possible by a contribution  from the company via James P. Flowers.

3) The supply of steel fiber was made possible by a contribution from N.V. BEKAERT S.A.